GREEN INHIBITION OF ALUMINIUM CORROSION IN 0.9 M HCL USING DIOSCOREA BULBIFERA EXTRACT: ROLE OF TEMPERATURE AND ADSORPTION MECHANISM

### Abstract

The slow degradation of metals brought on by chemical or electrical interactions with their surroundings, especially in acidic conditions, is known as corrosion. In this study, weight loss, thermodynamic, kinetic, adsorption, and electrochemical methods were used to examine the effect of  Dioscorea bulbifera leaf extract on corrosion with aluminum in 0.9 M HCl. According to the weight loss data, inhibitory efficacy rises with extract concentration but falls with temperature. With an inhibitory efficacy of almost 60%, the corrosion rate dropped dramatically from 0.046 mm yr⁻¹ in the blank to 0.039 mm yr⁻¹ at 0.6 g of extract at 303 K, demonstrating efficient adsorption and protective coating development. However, corrosion rates rose and efficiency decreased at higher temperatures (313–323 K), indicating temperature-sensitive inhibition. The activation energy increased from 32.890 to 40.220 kJ mol⁻¹ according to thermodynamic analysis, indicating that the inhibitor increases the corrosion energy barrier. A spontaneous adsorption process, mostly via physisorption, indicated negative Gibbs free energy values. According to adsorption studies, the system is best described by the Langmuir isotherm, suggesting monolayer adsorption. According to kinetic analysis, corrosion exhibits first-order kinetics, with lower rate constants and a longer half-life when the inhibitor is present. Electrochemical studies, which demonstrated a notable drop in corrosion current density and corrosion rate with increasing extract concentration, further validated inhibitory efficacy. In conclusion, aluminum corrosion in acidic media is well inhibited by Dioscorea bulbifera extract, particularly at lower temperatures.

Keywords: HCl, Corrosion, Green inhibitor, Thermodynamics, Kinetics Potentiodynamics

1.0 Introduction

A recurring problem in materials science and industrial processes is corrosion, which is the slow deterioration of metals as a result of their contact with harsh environments [1]. Aluminum's low density, strong mechanical properties, and superior conductivity make it one of the most popular engineering metals [2–3]. It is also prized for its capacity to create a thin oxide layer that, under typical circumstances, provides some corrosion protection [4]. However, this protective layer becomes fragile and dissolves in extremely acidic settings, such strong hydrochloric acid solutions, leaving the metal surface vulnerable to rapid assault [5]. Aluminum components are especially sensitive in sectors that utilize hydrochloric acid often, including acid pickling, descaling, and chemical cleaning, especially at higher acid concentrations when corrosion rates are greatly increased [6–7]. Corrosion inhibitors are frequently added to the corrosive medium to lessen this issue. By creating an adsorbed coating on the metal surface, these compounds slow down electrochemical processes and block active corrosion sites, which lowers the rate of metal dissolution [8]. Despite the previous effectiveness of inorganic inhibitors such chromates and phosphates, their usage is becoming less common because of their toxicity, persistence in the environment, and related health hazards [9]. As a result, there is increasing demand in safer and more ecologically friendly alternative inhibitors. In this regard, compounds produced from plants—often called "green inhibitors"—have become effective alternatives. These materials are appealing for large-scale applications because they are often easily accessible, non-toxic, and biodegradable [10]. The presence of naturally occurring organic components such flavonoids, tannins, alkaloids, and phenolic substances is primarily responsible for their efficacy [11]. These substances have electron-rich structures and functional groups that allow them to interact strongly with metal surfaces through adsorption processes [12]. Recent research has focused on Dioscorea bulbifera, a tropical plant with a rich phytochemical profile, because of its possible inhibitory qualities. It is anticipated that the leaf extract in particular will have active ingredients that can create a barrier of defense on aluminum surfaces in acidic situations. Despite the significant expansion of research on green corrosion inhibitors, significant limits still exist. The action of inhibitors in highly concentrated and aggressive systems, such 0.9 M HCl, is not well understood since a large majority of previous research have centered on relatively diluted acid media, frequently below 0.5 M HCl. Furthermore, a number of studies only employ gravimetric (weight loss) analysis, which is helpful but does not give enough details on the electrochemical processes at play. It is difficult to differentiate between anodic and cathodic inhibitory mechanisms in the absence of supplementary methods like potentiodynamic polarization. Furthermore, in many instances, the connection between inhibitor efficacy and surface shape has not been fully investigated. Although they are occasionally disregarded, surface analytical instruments like scanning electron microscopy (SEM) are crucial for verifying the creation and integrity of protective layers. The inadequate handling of thermodynamic factors related to the adsorption process is another crucial gap. Clarifying the nature of the interaction between inhibitor molecules and the metal surface and assessing the stability of the adsorbed layer under various conditions need an understanding of elements like activation energy, enthalpy, and entropy changes. Furthermore, despite its significance in assessing the effectiveness and usefulness of corrosion inhibitors, the combined impact of inhibitor concentration and exposure duration is frequently underreported. In light of this, the current study is to examine how effectively Dioscorea bulbifera leaf extract inhibits corrosion on aluminum in a very aggressive 0.9 M hydrochloric acid solution. The study's main goals are to measure corrosion rates and inhibition efficiencies using the weight loss method, analyze the system's electrochemical behavior using potentiodynamic polarization measurements, investigate surface alterations and film formation using SEM analysis, and assess thermodynamic parameters controlling the adsorption process. We will pay special attention to how changes in immersion time and inhibitor concentration affect the corrosion process and the extract's overall efficacy at various temperatures. This work is limited to laboratory-scale experiments in which aluminum samples are subjected to controlled acidic conditions both with and without the plant extract. To offer a thorough evaluation of inhibitor performance, a mix of gravimetric, electrochemical, and surface characterisation methods will be used. The study does not cover industrial implementation or long-term field evaluation, even though the results should provide insightful information on the corrosion protection mechanism.

2.0 Experimental

2.1 Plant Extraction

Leaves from the plant Discorea bulbifera were collected at the BUK agro facility's new location in Kano State's Gwale Local Government area. In compliance with the analytical approach, the plant leaves were gathered and dried beneath a shed [11]. Discorea bulbifera leaves were extracted using 99% pure ethanol as a solvent. For two weeks, 500 g of the pulverized powdered leaves were added to two liters of ethanol at a time, shaken occasionally, and filtered using Whatmann filter paper [12]. To get the concentrate crude extract, the solution was evaporated at 480C using a rotary evaporator, Model R-210 [13]. For use in future experiments, the crude extract was dried, kept in a clean bottle, and carefully covered.

2.2 Preparation of inhibitor solution in 0.9M HCl

In order to conduct the experiment, 0.2, 0.4, and 0.6 gL-1 concentrations of the extract were injected into 0.9M HCl, which was made by weighing 0.2, 0.4, and 0.6 g of the extract and dissolving each in 5 ml of ethanol. The extract was then individually transferred into a 1-liter volumetric flask and made with 0.9M HCl solution [14]. Equation (1) was used to solve the corredent.

C1V1 = C2V2                                                                                                          (1)

Where: C1   = Concentration of stock solution, V1    ==    volume of stock solution to be measured, C2    =   concentration to be prepared, V2     =   volume to be prepared

2.3 Preparation of the Aluminium Coupons

The 1 x 1 x 0.11 mm aluminum sheet utilized in this investigation was purchased at the Kofar Ruwa Market in Kano, Nigeria. For a smoother surface, the sheet was physically polished and abraded using silicon carbide emery paper (120, 400, 800, and 1000 grade). It was then degreased by washing in ethanol, dried in acetone, and kept in a desiccator.

2.4 Weightloss Experiment

The coupons were submerged in 0.9M HCl for four hours, both with and without inhibitors, and they were cleaned every hour to measure the coupons' weight loss throughout that time. Weight was measured both before and after immersion. This test was carried out in 100 mL at 303, 313, and 333 K under complete immersion circumstances. The recovered coupons underwent proper cleaning, drying, and reweighing. The difference between the coupons' initial weight and their current weight was considered the weight loss. Every test was conducted in duplicate, and data was collected. Subsequent computations utilized the average results from each experiment [15].

From the initial and final weights of mild steel, the weight loss (ΔW), corrosion rate (gh-1cm2), inhibition efficiency and the degree of surface coverage (θ) were calculated as shown in equations 2-4.

%IE = (1-W1W2)×100										(2)

θ   =  1-W1W2											(3)

CR (g/hcm-2)   =  ∆WAt										(4)

From the expression, W1 and W2 are the weight losses ΔW (g) for mild steel in the presence and absence of Sarcocephalus latifolius extract respectively, θ is the degree of surface coverage of the inhibitor, A is the area of the metal coupon (in cm2), t is the time taken for the corrosion in hours and ΔW is the W2 - W1 is the weight loss of mild steel after period, t. [1].

2.5 Thermodynamic Calculations

Enthalpy is the sum of the internal energy of the system plus the product of the pressure of the gas in the system and its volume while entropy is the measure of disorderliness of a system [16]. The thermodynamic parameters for the enthalpy of adsorption and entropy of the inhibitors on the (∆Hads) and (ΔSads) in the presence and absence of inhibitors was calculated using the transition state equation (29) [17-18].

CRT= RNh  exp∆sads2,303R =exp-AHads2,303RT                                                                           (5)

Where N is the Avogadro’s number (6.02252 x 1023 mol-1) and he is the Plank’s constant (6.626176 × 1034 Js) while other parameters have their usual definition. A plot of log (CRT) versus I/T gave a straight line with a slope equal to (-AHads2,303RT) and an intercept of log (RNh+ (∆Sads2,303R) from adsorption (Kads) of Bolanites aegyptiaca is related to the free energy of adsorption according to equation (3.4) [19].

The free energy of adsorption (ΔGads) was calculated using: ΔGads = -RTIn(Kads55.5)                     							(6)

where (Kads) is the adsorption equilibrium constant obtained from adsorption isotherm models. These calculations provided insight into the nature and spontaneity of the inhibition process.

3.6: Kinetic Studies

The kinetic of Aluminium corrosion in Hydrochloric acid solution was studied by fitting data obtain from weight loss experiment into different kinetic equation of zero first and second orders. As derived by equation 7-11.

dxdt     =  k1 (ao-x) 										(7)

Rearrangement of the equation 7 produces equation 8 and upon integration of equation 8 yield equation 9 respectively. From the equations derived k1 is the first order rate constant.

dx/(ao-x)   =   k1 dt										(8)

-ln(ao-x)   =  k1 t 										(9)

-log (∆w)   =  k1 t2.303										(10)

The half-life equation is obtained by fitting the value of the k1 constant in to the half-life equation as shown in equation 11

t1/2   = 0.693k1											(11)

A plot of –log (∆w) on the vertical axis to time, t at the horizontal axis, a linear graph was obtained and the values of the kinetic parameters obtain from the graphs

2.7 Potentiodynamic polarization experiment

A typical three-electrode electrochemical cell was used in a regular laboratory setup to conduct the potentiodynamic polarization experiment. The working electrode was aluminum coupons that had been mechanically polished, degreased using ethanol, rinsed with distilled water, and let to air dry. The reference electrode was a saturated calomel electrode (SCE), and the counter electrode was a platinum rod. The electrolyte was a 0.6 M hydrochloric acid solution with and without different amounts of leaf extract from Dioscorea bulbifera. The system was given 30 minutes to settle at open circuit potential (OCP) before measurements. The voltage was then swept from −250 mV to +250 mV against OCP at a scan rate of 1 mV/s in order to acquire potentiodynamic polarization curves. Tafel extrapolation was used to get corrosion current density and corrosion potential estimates for further study.

3.0 Result and discussion

3.1 Weight loss

Table 1 present Weight loss Δw (g), Corrosion rate (CR), Surface coverage (Ө) and inhibition efficiency (%IE) of various concentration of in 0.9M HCl solutions for 4hours, the weight loss data show that temperature and extract concentration have a major impact on aluminum corrosion behavior as also demonstrated in Figure 1 and 2 of the weight loss. At 303 K, the inhibition efficiency (%IE) marginally rises to almost 60%, while the corrosion rate (CR) drops from 0.046 mm yr⁻¹ in the blank to 0.039 mm yr⁻¹ at 0.6 g of extract. This suggests that the inhibitor molecules successfully bind on the aluminum surface, creating a barrier that lessens the breakdown of metal [15]. At this temperature, significant adsorption is supported by the comparatively high surface coverage ( ≈ 0.60) [16]. The inhibitor still functions rather well at 313 K, despite the fact that corrosion rates are often greater than at 303 K because of increased kinetic energy and improved reaction speeds [17]. The %IE stays between 45 and 51%, indicating that the adsorbed film is stable [17]. The which lower effectiveness as compared to 303 K, however, suggests that certain adsorbed molecules start to desorb at higher temperatures, weakening the protective barrier. Higher CR readings and noticeably lower %IE (12–31%) indicate that corrosion becomes more noticeable at 323 K [18]. The inhibitor film is less stable at higher temperatures, as evidenced by the sharp decline in inhibitory effectiveness.

This behavior implies that the adsorption process is mostly physical (physisorption), which is sensitive to temperature and becomes weaker as the temperature rises because inhibitor molecules desorb from the metal surface [1,19]. By increasing surface coverage, a higher extract concentration enhances inhibitory performance at lower temperatures. Nevertheless, efficiency decreases with rising temperature, demonstrating the temperature-dependent nature of the adsorption process and demonstrating that corrosion prevention works better in mildly heated environments [20]. This is also demonstrated in Figure 1 which show the effect of temperature on the weightloss of the corrosion process.

Table 1: Weight loss values

| Conc extract (g) | 303K |  |  |  |  |  | 313K |  |  | 323K |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ΔW(g) | CR | Ө | % IE | ΔW(g) | CR | Ө | % IE | ΔW(g) | CR | Ө | % IE |
| 0.0 | 1.359 | 0.046 | 0.576 | 58 | 1.123 | 0.057 | 0.510 | 51 | 0.546 | 0.065 | 0.311 | 31 |
| 0.2 | 1.302 | 0.045 | 0.587 | 59 | 0.812 | 0.055 | 0.451 | 45 | 0.507 | 0.066 | 0.314 | 31 |
| 0.4 | 1.252 | 0.042 | 0.602 | 60 | 0.748 | 0.050 | 0.454 | 45 | 0.138 | 0.063 | 0.120 | 12 |
| 0.6 | 1.157 | 0.039 | 0.603 | 60 | 0.669 | 0.046 | 0.449 | 45 | 0.226 | 0.059 | 0.198 | 19 |

Fig. 1: Variation of weight-loss with time of the corrosion inhibition of aluminium with temperature at 0.9HCl

| 303K | 313K | 323K |
| --- | --- | --- |

Fig 2: Variation of weight loss with time of Aluminium immersed in different concentrations of extract in 0.9M HCl at 303-323K

3.2 Thermodynamics

Using equations 5 and 6, Table 2 displays the data derived from the corrosion process. The thermodynamic and kinetic parameters for aluminum dissolving in 0.9 M HCl offer crucial information about the Dioscorea bulbifera extract's inhibitory mechanism. At 0.6 g extract concentration, the activation energy (ΔEa) gradually rises from 32.890 kJ mol⁻¹ in the blank solution to 40.220 kJ mol⁻¹. This increase in activation energy suggests that the inhibitor's presence produces an energy barrier to the corrosion process, making the dissolving of aluminum more challenging. According to Iorhuna and Ayuba 2022, this implies that inhibitor molecules are adsorbed onto the metal surface, creating a barrier that prevents mass transit and charge transfer [21].

A physical adsorption (physisorption) mechanism, in which the inhibitor inhibits corrosion by blocking active sites instead of creating strong chemical interactions, is likewise characterized by an increase in ΔEa. Similarly, when the inhibitor concentration rises, the enthalpy of activation (ΔHa) gradually increases from 0.161 to 0.187 kJ mol⁻¹. The endothermic dissolving process, which necessitates energy input for corrosion, is confirmed by the positive values of ΔHa [22]. The concept that the inhibitor increases the energy needed for aluminum oxidation and slows the corrosion response is further supported by the rise in ΔHa in the presence of the extract [23].

At all doses, the entropy of activation (ΔS) stays at −0.197 kJ mol⁻¹. Similar to Fiori-Bimbi, et al 2022[24], The transition state is more ordered than the reactants, as indicated by the negative value, which shows a decrease in disorder during the production of the activated complex. The interaction of inhibitor molecules with aluminum ions at the interface, which results in a more organized system, can account for this [25]. Dioscorea bulbifera extract prevents corrosion by adsorption, raising the energy barrier and creating an ordered protective coating on the aluminum surface, as confirmed by the rise in ΔEa and ΔHa and the negative ΔS [25].

Table 2: Energy parameters for the dissociation of Al in HCl in the absence and presence of Discorea Bulbifera

| Corrodent | Extract Conc (g) | ΔEa(kJmol-1) | ΔHa(kJmol-1) | ΔS(kJmol-1) |
| --- | --- | --- | --- | --- |
| 0.9MHCl | Blank | 32.890 | 0.161 | -0.197 |
|  | 0.2 | 35.150 | 0.168 | -0.197 |
|  | 0.4 | 37.390 | 0.177 | -0.197 |
|  | 0.6 | 40.220 | 0.187 | -0.197 |

The adsorption findings demonstrate that the Langmuir adsorption isotherm is mostly followed by the interaction of Dioscorea bulbifera extract with the aluminum surface in 0.9 M HCl, particularly at 303 K and 313 K, where the correlation coefficient (R² = 1.0000) exhibits an excellent match as shown in Table 3. This implies that there is no interaction between the adsorbed species and monolayer adsorption occurs on a homogenous surface [26]. However, the lower R2 value (0.6585) at 323 K shows a departure from ideal Langmuir behavior, most likely as a result of partial desorption at higher temperatures or greater surface heterogeneity [27].

From 8.0600 at 303 K to 172.41 at 313 K, the adsorption equilibrium constant (Kads) rises dramatically before falling to 16.890 at 323 K. Stronger adsorption and increased durability of the inhibitor layer at a moderate temperature are shown by the high Kads value at 313 K. The following drop at 323 K indicates that heat agitation weakened adsorption, causing inhibitor molecules to desorb [28]. At all temperatures (−15.378 to −23.858 kJ mol⁻¹), the Gibbs free energy of adsorption (ΔG) values are negative, indicating that the adsorption process is spontaneous [24].

The adsorption process is mostly physical (physisorption), including electrostatic interactions between inhibitor molecules and the charged aluminum surface, as shown by the amount of ΔG (between −20 and 0 kJ mol⁻¹) [21].

Table 3: Adsorption Isotherm for the Adsorption of Discorea Bulbifera Extract Onto Al Surface in 0.9MHCl

| ISOTHERMS | TEMP(K) | PARAMETERS |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Intercept | Slope | R2 | Kads | ΔG (Kjmol-1) |
| Langmuir | 303 | 1.6359 | 0.0124 | 1.0000 | 8.0600 | -15.378 |
|  | 313 | 2.2330 | 0.0058 | 1.0000 | 172.41 | -23.858 |
|  | 323 | 5.9677 | 0.0592 | 0.6585 | 16.890 | -18.380 |
| Temkin | 303 | 0.0358 | 0.613 | 0.8868 | 51.530 | -3.2200 |
|  | 313 | 0.0030 | 0.4498 | 0.0912 | 1.4450 | -3.8300 |
|  | 323 | 0.2845 | 0.0857 | 0.4993 | 25.180 | -1.4500 |

Table 4: Kinetic parameters for the corrosion of Aluminium in 0.9 M HCl containing various concentrations of Discorea bulbifera varying Temperatures.

| TEMP (K) | C0NC.(gL-1) | 0.9M |  |  |
| --- | --- | --- | --- | --- |
| 303 |  | k1 | t1/2 | R2 |
|  | 0.0 | 0.785 | 0.883 | 0.983 |
|  | 0.2 | 0.781 | 0.887 | 0.997 |
|  | 0.4 | 0.777 | 0.892 | 0.971 |
|  | 0.6 | 0.779 | 0.899 | 0.991 |
| 313 | 0.0 | 0.906 | 0.765 | 0.987 |
|  | 0.2 | 0.901 | 0.769 | 0.890 |
|  | 0.4 | 0.878 | 0.789 | 0.976 |
|  | 0.6 | 0.867 | 0.799 | 0.945 |
| 323 | 0.0 | 1.027 | 0.675 | 0.765 |
|  | 0.2 | 1.021 | 0.679 | 0.998 |
|  | 0.4 | 1.016 | 0.682 | 0.812 |
|  | 0.6 | 1.007 | 0.688 | 0.876 |

The kinetic results for aluminum corrosion in 0.9 M HCl with Dioscorea bulbifera extract present provide crucial information about the inhibitor's effectiveness and reaction mechanism. The comparatively strong correlation values (R² = 0.76–0.998) in Table 4 show that the corrosion process follows first-order kinetics at all temperatures. This implies that the concentration of the reactive species at the metal surface is the main factor influencing the rate of aluminum dissolution [29]. The half-life (t₁/₂) somewhat rises at 303 K, although the rate constant (k₁) decreases slightly from 0.785 in the blank to 0.777–0.779 after inhibitor addition.

This suggests that by prolonging the time needed for substantial metal breakdown, the extract will slow down the corrosion response [30].  But when the inhibitor concentration rises, k₁ steadily falls and t₁/₂ rises. This shows that by slowing down the pace of reaction, the inhibitor is still effective even at high temperatures [31]. Improved surface covering and the creation of a protective barrier that postpones metal breakdown are suggested by the steady rise in half-life with inhibitor concentration. The comparatively smaller variations at higher temperatures, however, suggest that the inhibitor molecules partially desorb, which lowers effectiveness [31].

Table 5 Linear Polarization Resistance Data for Discorea Bulbifera extract in Various Acidic Medium.

| Extract Concentration (gL-1) | icorr(μAcm-2) | Ecorr(mV) | Ba(mVdec-1) | Bc(mVdec-1) | C.R(mmpy-1) | µρ(%) |
| --- | --- | --- | --- | --- | --- | --- |
| 0.0 0.2 0.4 0.6 | 9917.755 5972.380 4682.323 2543.141 | -710.480 -645.682 -630.477 -623.313 | 189.200 214.800 234.700 151.400 | 137.4 214.8 231.5 153.2 | 21.450 9.1340 5.6209 0.1843 | - 39.78 52.79 74.36 |

Fig. 3: Overlaid Tafel plot of the study

As observed in Table 5 and Figure 3 of the Tafel, the electrochemical data obtained in 0.9 M HCl unequivocally demonstrate that both the aggressive acid concentration and the inhibitor concentration greatly impact the corrosion behavior of aluminum. The extremely high corrosion current density (icorr) of 9917.755 μA cm⁻² in the uncontrolled solution indicates that the high acid strength encourages quick metal breakdown [32]. Dioscorea bulbifera extract, however, causes icorr to gradually drop to 2543.141 μA cm⁻² at 0.6 g L⁻¹, demonstrating that inhibitor concentration has a potent moderating effect even in a highly corrosive media.

The corrosion potential (Ecorr) slightly increased from −710.480 mV to −623.313 mV, indicating that the inhibitor is still a mixed-type inhibitor that affects both anodic and cathodic processes [21,33]. Because both processes are greatly enhanced in 0.9 M HCl, this feature is very significant; the extract concurrently lowers their rates by adsorption on the aluminum surface. With increasing inhibitor concentration, the inhibition efficacy rises from 39.78% to 74.36%, while the corrosion rate falls sharply from 21.450 mm yr⁻¹ to 0.1843 mm yr⁻¹. This suggests that a larger concentration of extract improves surface coverage, creating a more compact, acid-resistant coating is result is similar to Ibrahim et al 2025 [26].

| Uninhibited | nhibited |
| --- | --- |

Figure 4: SEM for inhibited and Unihibited Aluminium sample in Discorea bulbifera extract

In Figure 4, the surface shows dark patches and roughness after being submerged in Dioscorea bulbifera leaf extract in 0.9M HCl, which indicates partial pitting corrosion. The uneven distribution of these pits indicates a localized acid attack that the extract weakened [34-35]. Polyphenols and flavonoids, among other plant chemicals, adsorb onto the metal to produce a partial protective coating that lessens corrosion but does not completely stop it. Both corrosion products and inhibitor compounds are suggested by clustered deposits [36-39]. All things considered, the extract offers modest inhibition, delaying corrosion and maintaining aluminum surface deterioration in acidic environments.

Conclusion

In Conclusion, the findings clearly show that Dioscorea bulbifera leaf extract is a potent corrosion inhibitor for aluminum in 0.9 M HCl, with temperature and inhibitor concentration having a significant impact on performance. The findings on corrosion rate and weight loss demonstrate that inhibitory efficiency rises with extract content, peaking at 0.6 g, especially at 303 K, when surface coverage is greatest. But when the temperature rises, the efficiency drastically drops, indicating that thermal desorption causes the protective coating to become less stable. When the inhibitor is present, thermodynamic data show an increase in enthalpy and activation energy, suggesting the creation of an energy barrier that slows down the breakdown of aluminum. The development of an ordered adsorbed layer is further suggested by the negative entropy values.

At lower temperatures, adsorption tests verify that the process follows the Langmuir isotherm; spontaneous and mostly physical adsorption is indicated by negative Gibbs free energy values. While electrochemical data verify a mixed-type inhibition mechanism with a notable decrease in corrosion current density and rate, kinetic analysis demonstrates that the corrosion process follows first-order kinetics. Overall, the extract offers good protection in moderate the environment, but its effectiveness declines at higher temperatures because of the physisorption process.

Reference

- Berrissoul, A., Loukili, E., Mechbal, N., Benhiba, F., Guenbour, A., Dikici, B., Zarrouk, A., & Dafali, A. (2020). Anticorrosion effect of a green sustainable inhibitor on mild steel in hydrochloric acid. Journal of Colloid and Interface Science, 580, 740–752. https://doi.org/10.1016/j.jcis.2020.07.073

- Rizi, A., Sedik, A., Acidi, A., Rachedi, K. O., Ferkous, H., Berredjem, M., Delimi, A., Abdennouri, A., Alam, M., Ernst, B., & Benguerba, Y. (2023). Sustainable and green corrosion inhibition of mild steel. ACS Omega, 8(49), 47224–47238. https://doi.org/10.1021/acsomega.3c06548

- Khamis, E., Abdel-Gaber, A. M., Morshidy, M., & Mohamed, M. E. (2025). Eco-friendly inhibitors for corrosion protection of mild steel. Scientific Reports, 15(1), 42549. https://doi.org/10.1038/s41598-025-27271-8

- Nwoye, C. I., & Nwigwe, U. S. (2025). Novel green corrosion inhibitor for mild steel protection. Portugaliae Electrochimica Acta, 43(1), 1–15. https://doi.org/10.4152/pea.2025430102

- Ramesh, T., Suji, D., & Quraishi, M. A. (2022). Evaluation of greener corrosion-inhibiting admixtures. Arabian Journal for Science and Engineering, 47(10), 13451–13466. https://doi.org/10.1007/s13369-022-06873-8

- Mohammed, N. J., Yusop, M. R., & Othman, N. K. (2026). Green and nano-based corrosion inhibition strategies. npj Materials Degradation, 10(1), 16. https://doi.org/10.1038/s41529-025-00726-z

- Sedik, A., Lerari, D., Salci, A., et al. (2020). Dardagan fruit extract as eco-friendly inhibitor. Journal of Taiwan Institute of Chemical Engineers, 107, 189–200. https://doi.org/10.1016/j.jtice.2019.12.006

- Belakhdar, A., Ferkous, H., Djellali, S., et al. (2020). Polyphenols as green inhibitors. Colloids and Surfaces A, 606, 125458. https://doi.org/10.1016/j.colsurfa.2020.125458

- Kahlouche, A., Ferkous, H., Delimi, A., et al. (2022). Cytisus multiflorus extract corrosion inhibition. Journal of Molecular Liquids, 347, 118397. https://doi.org/10.1016/j.molliq.2021.118397

- Iorhuna, F., Ayuba, A. M., & Nyijime, T. A. (2024). Corrosion inhibition of mild steel using green inhibitors. Applied Journal of Environmental Engineering Science, 10(2), 1–15. https://doi.org/10.48422/IMIST.PRSM/ajees-v10i2.48140

- Verma, C., Ebenso, E. E., & Quraishi, M. A. (2020). Ionic liquids as green corrosion inhibitors. Journal of Molecular Liquids, 298, 111984. https://doi.org/10.1016/j.molliq.2019.111984

- Lgaz, H., Salghi, R., et al. (2020). Green corrosion inhibitors for steel. Journal of Materials Research and Technology, 9(2), 2973–2986. https://doi.org/10.1016/j.jmrt.2019.12.035

- Obot, I. B., & Madhankumar, A. (2020). Plant extracts as eco-friendly inhibitors. Surface Engineering and Applied Electrochemistry, 56(1), 1–12. https://doi.org/10.3103/S1068375520010094

- Quraishi, M. A., Chauhan, D. S., et al. (2020). Green corrosion inhibitors review. Journal of Molecular Liquids, 321, 114468. https://doi.org/10.1016/j.molliq.2020.114468

- Chauhan, D. S., et al. (2021). Expired drugs as green inhibitors. Journal of Molecular Liquids, 325, 115092. https://doi.org/10.1016/j.molliq.2020.115092

- Umoren, S. A., & Solomon, M. M. (2021). Synergistic corrosion inhibition. Journal of Industrial and Engineering Chemistry, 97, 1–17. https://doi.org/10.1016/j.jiec.2021.02.005

- Alaneme, K. K., & Olusegun, S. J. (2021). Green inhibitors for aluminium corrosion. Alexandria Engineering Journal, 60(3), 2743–2756. https://doi.org/10.1016/j.aej.2020.12.037

- Eddy, N. O., & Ebenso, E. E. (2021). Adsorption and corrosion inhibition studies. Journal of Materials Science, 56(12), 7452–7466. https://doi.org/10.1007/s10853-021-05692-0

- Abd El-Lateef, H. M., et al. (2021). Natural polymer inhibitors. Journal of Molecular Liquids, 337, 116431. https://doi.org/10.1016/j.molliq.2021.116431

- Singh, A., et al. (2022). Plant-based corrosion inhibitors. Materials Today Communications, 30, 103117. https://doi.org/10.1016/j.mtcomm.2022.103117

- Iorhuna Fater, & Ayuba, A. M. (2023). Mild steel corrosion inhibition in acidic media using Sarcocephalus latifolius leaves extract. Journal of Fundamental and Applied Sciences, 15(1).

- Verma, C., et al. (2022). Biomass-derived inhibitors. Green Chemistry Letters and Reviews, 15(2), 200–215. https://doi.org/10.1080/17518253.2022.2048123

- Fiori-Bimbi, M. V., et al. (2022). Natural extracts corrosion inhibition. Electrochimica Acta, 404, 139760. https://doi.org/10.1016/j.electacta.2021.139760

- Lebrini, M., et al. (2022). Eco-friendly corrosion inhibitors. Corrosion Science, 198, 110131. https://doi.org/10.1016/j.corsci.2021.110131

- Solomon, M. M., et al. (2022). Green inhibitors for steel corrosion. Journal of Materials Research and Technology, 17, 1925–1940. https://doi.org/10.1016/j.jmrt.2022.01.089

- Ibrahim, M., Ayuba, A. M., Hussein, M., & Iorhuna Fater (2025). Corrosion inhibition of mild steel in 0.3 M hydrochloric acid solution using Urena lobata leaves extract. Applied Journal of Environmental Engineering Science, 10(4). https://doi.org/10.48422/IMIST.PRSM/ajees-v10i4.49700

- Yadav, M., et al. (2022). Green inhibitors adsorption studies. Journal of Molecular Liquids, 350, 118521. https://doi.org/10.1016/j.molliq.2022.118521

- Kaya, S., et al. (2023). Theoretical study of green inhibitors. Journal of Molecular Liquids, 368, 120636. https://doi.org/10.1016/j.molliq.2022.120636

- Iorhuna F., Ayuba AM. Adsorptive, Kinetic and Thermodynamic Investigations of Sarcocephalus latifolius Leaves Extract as Corrosion Inhibitor on Alloy Steel in 0.6M HCl Solution. Alger. J. Eng. Technol. 2022; 7:83-91. http://www.jetjournal.org/index.php/ajet/article/download/258/92

- Kumar, A., et al. (2023). Plant extract corrosion inhibition. Surface Interfaces, 34, 102345. https://doi.org/10.1016/j.surfin.2022.102345

- Ogunleye, O. O., et al. (2023). Eco-friendly inhibitors for aluminium. Heliyon, 9(5), e15987. https://doi.org/10.1016/j.heliyon.2023.e15987

- Loto, R. T., et al. (2023). Corrosion inhibition of steel using plant extracts. Results in Engineering, 17, 100950. https://doi.org/10.1016/j.rineng.2023.100950

- Ebenso, E. E., et al. (2023). Adsorption behavior of green inhibitors. Journal of Adhesion Science and Technology, 37(8), 985–1002. https://doi.org/10.1080/01694243.2022.2040198

- Verma, C., Ebenso, E. E., & Quraishi, M. A. (2020). Plant extracts as corrosion inhibitors for metals. Journal of Molecular Liquids, 312, 113377. https://doi.org/10.1016/j.molliq.2020.113377

- Singh, P., et al. (2024). Green inhibitors in acidic media. Journal of Molecular Liquids, 385, 122214. https://doi.org/10.1016/j.molliq.2023.122214

- Verma, C., et al. (2024). Advances in green corrosion inhibitors. Progress in Organic Coatings, 184, 107698. https://doi.org/10.1016/j.porgcoat.2023.107698

- Okafor, P. C., et al. (2024). Plant extracts for corrosion inhibition. Chemical Papers, 78(4), 2103–2115. https://doi.org/10.1007/s11696-023-03045-1

- Hassan, H. H., et al. (2024). Eco-friendly inhibitors for oilfield applications. Journal of Petroleum Science and Engineering, 232, 111948. https://doi.org/10.1016/j.petrol.2023.111948

- Abdallah, M., et al. (2025). Natural compounds as corrosion inhibitors. Journal of Molecular Liquids, 402, 123456. https://doi.org/10.1016/j.molliq.2024.123456

- Sharma, S., et al. (2025). Bio-based corrosion inhibitors. Materials Chemistry and Physics, 310, 127456. https://doi.org/10.1016/j.matchemphys.2024.127456